## Slide 1
NUMERICAL MODELING OF FRICTION STIR WELDING PROCESSES
María de los Angeles González
Barcelona, November 11th 2015

## Slide 2
INTRODUCTION
FSW Process Sketch
Real FSW Process
[1]
[2]

## Slide 3
INTRODUCTION
Benefits and Advantages of FSW
Ability to join materials that are difficult to weld.
Low distortion and shrinkage.
No porosity.
No spatter.
[3]

## Slide 4
PROBLEM STATEMENT
2D Model
Program COMET- FWS provided by Prof. Michele Chiumenti
Data is given by SAPA company
Geometry, Materials, and velocities
Pre and postprocessor GID program
The results are visualize
The problem is solved
The model is built

## Slide 5
PROBLEM STATEMENT
Zones
Geometry
30
30
4
14.5
Units in mm
Plate
HAZ
Pin

## Slide 6
PROBLEM STATEMENT
Kinematic Framework
Initial Data
Eulerian
ALE
Lan

## Slide 7
PROBLEM STATEMENT
Plate and HAZ Properties- Aluminum 6063
Thermal Properties
Mechanical Properties
Bingham model
[4]

## Slide 8
PROBLEM STATEMENT
The specific heat, density and conductivity depend of temperature
PIN Properties-Steel
Chart: Specific Heat Cp
| 1 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1375 | 1458 | 2000
Specific heat | 426.054 | 485.524 | 532.022 | 565.122 | 604.85 | 665.538 | 768.707 | 1400 | 890.604 | 600.053 | 615.593 | 621.103 | 637.144 | 644.181 | 750 | 750
Chart: Density ρ
| 1 | 600 | 1100 | 1375 | 1430
 | 7830 | 7644 | 7561 | 7417 | 7266
The pin is considered rigid
Mechanical Properties
[5]

## Slide 9
PROBLEM STATEMENT
A transition between the surfaces was defined. From 0.01 mm to 1 mm.
Mesh Discretization

## Slide 10
RESULTS AND DISCUSSIONS
Temperature- Contour fill

## Slide 11
RESULTS AND DISCUSSIONS
Evolution of Temperature
2
1
Point 2
Point 1

## Slide 12
RESULTS AND DISCUSSIONS
Pressure- Contour fill

## Slide 13
RESULTS AND DISCUSSIONS
2
1
Point 2
Point 1
Evolution of Pressure

## Slide 14
CONCLUSIONS AND FUTURE WORK
The program generates stable and expected solutions for temperature and pressure.
A convergence analysis should be perform in order to choose the most suitable mesh.
The numerical results must be compare again the experimental data with the purpose to validate the model.
A sensibility analysis of FSW process parameters using simplified pin mesh discretization should be perform.

## Slide 15
REFERENCES [online]
“What is Friction Stir Welding (FSW)?” [online]. [Date of consultation: 10-11-2015]. Available in: http://www.mosaka.com/fsw/en/fsw/about_fsw.html
[1]
[2]
[3]
[4]
[5]
“CM: Case Modding” [online]. [Date of consultation: 10-11-2015]. Available in: http://www.techzine.nl/uploaded/4718_cab3ee96.jpg
“ Friction Stir Welding of Aluminum” [online]. [Date of consultation: 10-11-2015]. Available in:
http://www.youtube.com/watch?v=BQYLdw8W5wE
“Friction Stir Welding (FSW): Introduction” [online]. [Date of consultation: 10-11-2015]. Available in: http://aluminium.matter.org.uk/content/html/default.asp?catid=205&pageid=2144416862
“Welcome to Techno Engineering Co.” [online]. [Date of consultation: 10-11-2015]. Available in:http://www.indiamart.com/technoengineeringco/

## Slide 16
THANK YOU FOR YOUR ATTENTION