## Slide 1: Wood Concrete multifunctional LCA
Master project FS19 by Lukas Vögeli
Assisted by Francesco Pittau under the chair of Guillaume Habert
In collaboration with HEIA Fribourg
Notes: What is Wood concrete multifunctional LCA?
LCA = Life cycle assessment = tool to measure the environmental impact of something
Multifunctional: More than one function: Mechanical properties + insulation

## Slide 2: What is WooCon?
© D. Zwicky
Notes: WooCon = special concrete containing wood (sawdust) and bio-based materials (grape seeds, cherry pits, nutshell) = additives
In collaboration with HEIA Fribourg (Haute école of engineering and architecture Fribourg)
It was my job to do a LCA on WooCon in order to get a reference whether the product might be competitive from an environmental perspective and therefore suitable for the future construction market…

## Slide 3: Why multifunctional?
Mechanical properties
Thermal properties

## Slide 4: What is LCA?
Notes: LCA = Tool to assess the total environmental impact of something
1. Goals & scope definition  boundaries of the system (FU)
2. Life-cycle inventory  data collection (Input)
3. Impact assessment  environmental impact (Output)
4. Interpretation

## Slide 5: Objectives
Analysing and comparing WooCon on material level Functional unit (FU): 1 m3 of concrete
Analysing and comparing WooCon on structural level Functional unit (FU): 1 m2 of slab
Adding multifunctionality (thermal insulation)
Optimisation of material
Notes: So what exactly am I analysing?
It's all about the FU

## Slide 6: Objectives
Analysing and comparing WooCon on material level Functional unit (FU): 1 m3 of concrete
Analysing and comparing WooCon on structural level Functional unit (FU): 1 m2 of slab
Adding multifunctionality (thermal insulation)
Optimisation of material
Notes: So what exactly am I analysing with my LCA
It's all about the FU

## Slide 7: WooCon mix design
 |  | WooCon 06 | WooCon 10 | WooCon 12 | WooCon 13 | WooCon 14
Cement | [kg/m3] | ca. 475 | ca. 475 | ca. 475 | ca. 475 | ca. 475
Lime filler | [kg/m3] | ca. 400 | ca. 400 | ca. 400 | ca. 400 | ca. 400
Sawdust | [kg/m3] | ca. 100 | ca. 100 | ca. 100 | ca. 100 | ca. 100
Expanded glass | [-] | x | x | x | x | x
Water | [-] | x | x | x | x | x
Superplasticizer | [-] | x | x | x | x | x
Sand | [-] | x | - | - | - | -
Expanded clay | [-] | x | x | - | - | x
Grape seeds | [-] | - | x | x | x | x
Cherry pits | [-] | x | - | x | x | x
Nuthsell | [-] | - | - | x | - | -
Saturated density | [kg/m3] | 1660 | 1580 | 1600 | 1600 | 1550
Bulk density | [kg/m3] | 1411 | 1343 | 1360 | 1360 | 1318
Compressive strength | [MPa] | 18.0 | 18.9 | 13.6 | 12.9 | 14.0
E-Modulus | [GPa] | 9.1 | 8.5 | 6.1 | 6.5 | 6.2
Bio-based material | [M-%] | 4.0 | 2.3 | 10.4 | 10.2 | 6.6
Notes: MATERIAL LEVEL
Concrete: Aggregates (stone, gravel, sand) & paste (cement, water, additives, admixtures)
There are no real aggregates!
Just paste with lots of additives

## Slide 8: LCA modelling
Notes: It’s not rocket science and I can’t focus on modelling too much, I just want to let you know the key things:
Normal materials  SimaPro database
Biobased materials  More complicated
Key assumption: it’s a waste product (zero impact)
Only processes (Washing, Crushing, Drying, Sorting, Transport)

## Slide 9: WooCon GWP analysis
Chart: GWP of 1 m3 WooCon
| WooCon 6 | WooCon 10 | WooCon 12 | WooCon 13 | WooCon 14
Cement | 349.9984 | 363.9533 | 357.6511 | 358.6264 | 352.0991
Lime filler | 0.90298 | 0.93899 | 0.92296 | 0.92529 | 0.90833
Sawdust | 0.54446 | 0.56605 | 0.55613 | 0.55788 | 0.54796
Sand | 0.31452
Expanded clay | 14.3452 | 33.4875 | 14.4374
Expanded glass | 45.3111 | 47.1844 | 46.3648 | 46.4819 | 45.5452
Grape seeds | 3.2628 | 5.3557 | 8.5649 | 3.1555
Cherry pits | 6.107 | 6.2466 | 6.2573 | 6.1392
Nutshell | 6.5569
Water | 0.03925 | 0.040814 | 0.040101 | 0.0402 | 0.039468
Superplasticizer | 9.5972 | 10.0085 | 9.8714 | 9.8714 | 9.5972
Notes: Focus of this presentation: GWP (global warming potention) = [kg-CO2-eq.]
17 other impact categories measured with SimaPro:
Air and water pollutants, ozone depletion radiation, resource scarcity (land use, copper, oil), toxicity (Water, Land, Human health), acidification, biodiversity
GWP: 79% - 83% cement!

## Slide 10: Material level – Functional unit
 |  | WooCon 06 | WooCon 10 | WooCon 12 | WooCon 13 | WooCon 14 | C 30/37 | LC 16/18 | LC 12/13 | LC 8/9
Bulk density | [kg/m3] | 1411 | 1343 | 1360 | 1360 | 1318 | 2400 | 1200 | 1100 | 1000
Avg. compressive strength (cylinder) | [MPa] | 18.0 | 18.9 | 13.6 | 12.9 | 14.0 | 38 | 24 | 20 | 16
E-Modulus | [GPa] | 9.1 | 8.5 | 6.1 | 6.5 | 6.2 | 33.6 | 15 | 12.5 | 10
Functional unit: 1 m3 of concrete
Notes: Explain SIA C30/37
Functional unit – what do I compare
From now on I will proceed with WooCon 6…

## Slide 11: Material comparison
Chart: GWP of 1 m3 concrete
| C 30/37 | LC 16/18 | LC 12/13 | LC 8/9 | WooCon 6
 | 152.7606 | 338.7741 | 384.7801 | 429.1997 | 427.1601

## Slide 12: Material comparison
Chart: GWP of 1 m3 concrete
| C 30/37 | LC 16/18 | LC 12/13 | LC 8/9 | WooCon 6
Ordinary concrete | 152.7606
Lightweight concrete | 338.7741 | 384.7801 | 429.1997
Cement | 349.9984
Expanded glass | 45.3111
Expanded clay | 14.3452
Superplasticizer | 9.5972
Cherry pits | 6.107
Lime filler | 0.90298
Sawdust | 0.54446
Sand | 0.31452
Water | 0.03925
Notes: The lighter the concrete the higher its GWP per volume (higher cement content)
C  higher density and much higher strength
LC 16/18 & 12/13  slightly lower density and higher strength
LC 8/9  lower density and lower strength
So overall WooCon is worse but in the range of being competitive
Sand  Scarcity of resources (Espen will confirm)

## Slide 13: Outlook
Structural level
Thermal insulation
Notes: Structural level: 1 m^2 of slab instead of 1 m^3 of material
Adding multifunctionality  only small effect

## Slide 14: Optimisation
Chart: Cement sensitivty analysis
| CEM I | CEM II | CEM III | CEM IV
cement [kg] | 100 | 83.9805 | 59.516 | 44.7101
WooCon 6 [m3] | 100 | 86.8743 | 66.829 | 54.6976
Notes: 80% of GWP comes from cement (CEM I) !!!
Other optimisations of the mix design possible: Less expanded glass, more sawdust (and sand)

## Slide 15: Conclusion
WooCon potentially competitive
High uncertainties for bio-based materials
FU is crucial
Optimisation takes time (iterative process)
Notes: Everything depends on functional unit
Material level
Structural level
Global level  (1) Total structure
 (2) what if everybody uses WooCon?

## Slide 16: Thank you for your attention!

## Slide 17: Acknowledgement
ETH Zürich
Prof. Dr. Guillaume Habert
Dr. Francesco Pittau
Alina Galimshina
HEIA Fribourg
Prof. Dr. Daia Zwicky
Adam Attila Meszes