## Slide 1: Effect of partial replacement of sand by plastic waste on impact resistance of concrete: experiment and simulation
By
Maher Al-Tayeb, Mustafa Ismail, Hanafi Rade Mahmoud and B.A.Tayeh

## Slide 2: Overview
Background
Objective
Method
Results
  Workability
  Compressive strength
  Impact and bending strength
Conclusion

## Slide 3: Background
Disposal of waste plastic
Lack of good sand
Improve concrete properties
  Tensile strength
  Ductility
  Impact energy absorption
Earlier investigation on workability

## Slide 4: Objective
Study of impact load and the resulting displacement, and fracture energy, of concrete with plastic waste particles.
Numerical simulation to study the load-displacement behaviour of concrete with plastic waste particles, using FEM.

## Slide 5: Method
Materials
  45 MPa concrete with ordinary Portland cement
  Industrial waste polycarbonate (PW)
Experimental set-up
Finite element method

## Slide 6: Results
Slump values
Compressive strength
Elastic modulus
Chart: Slump (mm)
| 0 | 0.05 | 0.1 | 0.2
Slump (mm) | 160 | 130 | 110 | 80
Chart: Average compressive strength (KN)
| 0 | 0.05 | 0.1 | 0.2
Average compressive strength (KN) | 42 | 39 | 37 | 32
Chart: Average elastic modulus (GPa)
| 0 | 0.05 | 0.1 | 0.2
Average elastic modolus (GPa) | 29.24 | 28.37 | 26.59 | 24.65

## Slide 7: Tup, inertial and bending load

## Slide 8: Comparison between static and impact load
Chart: Peak bending load (N)
| 0 | 0.05 | 0.1 | 0.2
Static test | 4100 | 3606 | 3338 | 2923
Impact test | 8075 | 9809 | 11083 | 12704

## Slide 9: Comparison between experiment and FEM

## Slide 10: Conclusion
Increasing plastic content led to
  Decreased slump
  Decreased compressive strength
  Decreased static strength
  Increased impact strength
FEM modeling and simulations could predict the behavior of the concrete

## Slide 11: Reference
https://www.sciencedirect.com/science/article/pii/S2352012419301018